Synthesis routes and details

Intermediate 2[1,2], 4[3], was synthesized according to the literature procedures. All other reagents and solvents are used from commercial sources without further purification.

Synthesis of 5-bromo-N,N,6'-triphenyl-[1,1':2',1''-terphenyl]-3-amine (3).

Compound 3,5-dibromo-N,N-diphenylaniline (10.00 g, 24.81 mmol), 2-([1,1':3',1''-terphenyl]-2'-yl)-4,4,5,5-tetramethyl-1,3,2-dioxaborolane (2) (10.61g, 29.77 mmol), tetrakis(triphenylphosphine)palladium (2.87g, 2.48 mmol) and potassium hydroxide (6.96g, 124.03 mmol) were dissolved in tetrahydrofuran (100 mL) and H2O (20 mL) under a nitrogen atmosphere. After stirring at 80 °C for 15 h, the reaction was filtered, the solvent removed under vacuum condition, and then the residue purified by column chromatography on silica gel using petroleum ether/dichloromethane (3/1, v/v) as eluent, white solid was finally obtained. Yield: 7.65 g (55.81%). 1H NMR (400 MHz, DMSO-d6) δ 7.57-7.46 (m, 1H), 7.42-7.27 (m, 8H), 7.23 (dd, J = 8.4, 7.3 Hz, 4H), 7.12 -7.00 (m, 6H), 6.64 (dd, J = 7.1, 5.8 Hz, 6H), 6.50 (s, 1H). 13C NMR (101 MHz, Chloroform-d) δ 147.87, 146.96, 142.53, 141.65, 141.36, 137.64, 129.89, 129.38, 129.31, 128.34, 127.81, 127.73, 126.50, 125.22, 124.20, 124.10, 123.04, 121.70. MS (EI) m/z: 552.41 [M+]. Calcd for C36H26BrN: 552.52.

Synthesis of N3,N3''-(1,3-phenylene)bis(N3-(2,6-difluorophenyl)-N5,N5,6'-triphenyl-[1,1':2',1''-terphenyl]-3,5-diamine) (6).

Compound 3 (7.32 g, 13.24 mmol), N1,N3-bis(2,6-difluorophenyl)benzene-1,3-diamine (4) (2.00 g, 6.02 mmol), tris(dibenzylideneacetone)palladium(0) (551.15 mg, 601.86 μmol), dicyclohexyl(2',4',6'-triisopropyl-[1,1'-biphenyl]-2-yl)phosphane (573.85 mg, 1.2 mmol) and sodium tert-butoxide (3.47 g, 36.11 mmol) were dissolved in toluene (200 mL) under a nitrogen atmosphere. After stirring at 120 °C for 5 h, the reaction was filtered, the solvent removed under vacuum condition, and then the residue purified by column chromatography on silica gel using petroleum ether/dichloromethane (2/1, v/v) as eluent, white solid was finally obtained. Yield: 4.61 g (60.05%). 1H NMR (400 MHz, Chloroform-d) δ 7.45-7.36 (m, 6H), 7.30-7.29 (m, 6H), 7.19-7.07 (m, 18H), 6.93 -6.81 (m, 13H), 6.75 (s, 4H), 6.73 (s, 3H), 6.43 (d, J = 10.4 Hz, 4H), 6.36 (s, 2H), 6.28 (d, J = 7.1 Hz, 2H), 6.11 (s, 2H), 6.05 (d, J = 8.1 Hz, 2H). 13C NMR (101 MHz, Methylene Chloride-d2) δ 162.64, 162.59, 160.13, 160.08, 159.22, 159.16, 156.76, 156.71, 148.92, 148.61, 148.01, 147.31, 145.51, 143.14, 142.90, 142.79, 140.18, 131.24, 130.70, 130.32, 130.23, 128.93, 128.71, 128.26, 128.16, 128.06, 127.57, 124.78, 124.63, 124.54, 123.74, 123.59, 123.54, 121.64, 120.46, 120.31, 117.74, 113.81, 113.76, 113.58, 113.32, 113.21, 113.15, 113.04, 112.98, 110.06, 108.43.MS (EI) m/z: 1275.81 [M+]. Calcd for C90H62F4N4:1275.51.

Synthesis of N3,N3''-(1,3-phenylene)bis(N3,N5,N5,6'-tetraphenyl-[1,1':2',1''-terphenyl]-3,5-diamine) (7)

Using a similar synthetic procedure for compound 6, white solid was finally obtained. Yield: 3.6 g (59.08%). 1H NMR (400 MHz, Methylene Chloride-d2) δ 7.47-7.27 (m, 20H), 7.16-7.12 (m, 12H), 7.10 (s, 2H), 7.07-7.02 (m, 4H), 6.95-6.88 (m, 5H), 6.85-6.81 (m, 2H), 6.72 (d, J = 7.9 Hz, 8H), 6.62-6.53 (m, 5H), 6.42-6.30 (m, 6H), 6.22 (d, J = 8.1 Hz, 2H). 13C NMR (101 MHz, Methylene Chloride-d2) δ 147.82, 147.65, 147.37, 147.26, 147.12, 142.06, 141.63, 141.42, 138.99, 129.99, 129.64, 128.94, 128.89, 128.80, 127.61, 127.35, 126.28, 123.44, 122.88, 122.65, 122.57, 122.21, 121.76, 119.37, 119.03, 118.30, 29.69. MS (EI) m/z: 1203.67 [M+]. Calcd for C90H66N4: 1203.55.

Synthesis of DTPF-ν-DABNA.

Boron tribromide (8.16 mL, 84.67 mmol) was added to a solution of Compound 6 (4.5 g, 3.53 mmol) in o-dichlorobenzene (60 mL) at room temperature under a nitrogen atmosphere. After stirring at 200 °C for 20 h, the reaction mixture was allowed to cool to room temperature. After addition of N,N-diisopropylethylamine (55.31 mL, 317.52 mmol) at 0 °C, the solvent was removed in vacuo, and then the residue purified by column chromatography on silica gel using petroleum ether/dichloromethane (2/1, v/v) as eluent, orange solid was finally obtained. Yield: 2.73 g (59.94%). 1H NMR (400 MHz, Methylene Chloride-d2) δ 10.43 (s, 1H), 9.16 (d, J = 7.8 Hz, 2H), 7.57 (d, J = 7.7 Hz, 6H), 7.46 (t, J = 7.0 Hz, 2H), 7.43-7.32 (m, 6H), 7.30 (d, J = 7.2 Hz, 4H), 7.22-7.07 (m, 12H), 6.98 -6.83 (m, 16H), 6.71 (d, J = 7.6 Hz, 2H), 5.86-5.76 (m, 4H), 5.64 (s, 1H). 13C NMR (101 MHz, Methylene Chloride-d2) δ 160.94, 158.45, 158.41, 149.30, 147.64, 145.85, 144.38, 143.71, 141.84, 141.68, 141.63, 139.36, 134.97, 131.01, 130.94, 130.27, 129.52, 129.33, 128.14, 127.69, 127.33, 126.21, 120.03, 117.18, 112.90, 112.68, 111.83, 108.03, 98.72. MS (EI) m/z: 1291.35 [M+]. Calcd for C90H56B2F4N4: 1291.08.

Synthesis of DTP-ν-DABNA.

Using a similar synthetic procedure for DTPF-ν-DABNA, orange solid was finally obtained. Yield: 1.8 g (51.26%). 1H NMR (400 MHz, Methylene Chloride-d2) δ 10.42 (s, 1H), 9.17 (d, J = 6.0 Hz, 2H), 7.62-7.53 (m, 6H), 7.47-7.42 (m, 2H), 7.40-7.27 (m, 14H), 7.18 (d, J = 7.3 Hz, 12H), 6.94-6.85 (m, 12H), 6.69 (d, J = 8.6 Hz, 2H), 6.61 (d, J = 6.3 Hz, 4H), 5.73 (d, J = 17.8 Hz, 4H), 5.55 (s, 1H). 13C NMR (101 MHz, Methylene Chloride-d2) δ 150.00, 147.68, 145.87, 145.75, 143.58, 143.01, 141.90, 141.79, 141.67, 141.28, 139.68, 134.97, 130.94, 130.76, 130.54, 130.32, 129.71, 129.55, 129.48, 128.04, 127.67, 127.57, 127.25, 126.03, 124.14, 119.86, 117.05, 114.96, 110.38, 110.01, 103.05. MS (EI) m/z: 1219.28 [M+]. Calcd for C90H60B2N4: 1219.12.

Figure S1. 1H NMR and 13C NMR spectrum of compound 4.

Figure S2. 1H NMR and 13C NMR spectrum of compound 6.

Figure S3. 1H NMR and 13C NMR spectrum of compound 7.

Figure S4. 1H NMR and 13C NMR spectrum of DTPF-ν-DABNA.

Figure S5. 1H NMR and 13C NMR spectrum of compound DTP-ν-DABNA.

Figure S6. Calculation results of (a) ν-DABNA, (b) 4F-ν-DABNA and (c) ν-DABNA without diphenylamine

Figure S7. Packing mode of DTPF-ν-DABNA (a) and DTP-ν-DABNA (b).

Figure S8. Excited states of DTPF-ν-DABNA and DTP-ν-DABNA.

Figure S9. Excited states of ν-DABNA and 4F-ν-DABNA.

Figure S10. TGA of DTPF-ν-DABNA (a) and DTP-ν-DABNA (b), CV (c) curve of DTPF-ν-DABNA and DTP-ν-DABNA.

Figure S11. Absorption and fluorescence spectra of (a, c) DTPF-ν-DABNA and (b, d) DTP-ν-DABNA in various solvents (toluene, tetrahydrofuran, N,N-Dimethylformamide, dichloromethane, trichloromethane, 1,4-Dioxane and n-Hexane).

Figure S12. Fluorescence spectra of  DTPF-ν-DABNA and DTP-ν-DABNA (a) PPF (2 wt% doped film) and (b) neat film , transient spectra of (c) DTPF-ν-DABNA and (d) DTP-ν-DABNA in PPF (2 wt% doped film) at different temperatures from 77 to 300 K.

Figure S13. Energy-level diagram and chemical structures of the materials for the OLEDs based on DTPF-ν-DABNA and DTP-ν-DABNA as MR-TADF emitters.

Figure S14. Current efficiency (CE) versus power efficiency (PE) versus luminance characteristics.

Figure S15. Device lifetime of DTPF-ν-DABNA and DTP-ν-DABNA.

Table S1. Crystal parameters for DTPF-ν-DABNA and DTP-ν-DABNA.

| Identification code | DTPF-ν-DABNA | DTP-ν-DABNA |
| --- | --- | --- |
| Empirical formula | C90H56B2F4N4 | C90H60B2N4 |
| Formula weight | 1291 | 1219.04 |
| Temperature/K | 170 | 100 |
| Crystal system | monoclinic | triclinic |
| Space group | P21/c | P-1 |
| a/Å | 17.1615(8) | 13.8558(11) |
| b/Å | 14.0010(6) | 16.8935(15) |
| c/Å | 33.9349(16) | 21.1023(18) |
| α/° | 90 | 102.224(3) |
| β/° | 101.338(2) | 104.161(2) |
| γ/° | 90 | 108.425(2) |
| Volume/Å3 | 7994.7(6) | 4313.7(6) |
| Z | 4 | 2 |
| ρcalcg/cm3 | 1.073 | 0.939 |
| μ/mm-1 | 0.068 | 0.054 |
| F(000) | 2680 | 1276 |
| Crystal size/mm3 | 0.15 × 0.08 × 0.05 | 0.12 × 0.07 × 0.04 |
| Radiation | MoKα (λ = 0.71073) | MoKα (λ = 0.71073) |
| 2Θ range for data collection/° | 3.828 to 51.422 | 3.884 to 52.884 |
| Index ranges | -20 ≤ h ≤ 20, -17 ≤ k ≤ 16, -39 ≤ l ≤ 41 | -15 ≤ h ≤ 17, -21 ≤ k ≤ 20, -26 ≤ l ≤ 26 |
| Reflections collected | 51828 | 45482 |
| Independent reflections | 14904 [Rint = 0.0801, Rsigma = 0.0827] | 17247 [Rint = 0.0683, Rsigma = 0.0938] |
| Data/restraints/parameters | 14904/0/901 | 17247/0/865 |
| Goodness-of-fit on F2 | 1.039 | 1.048 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0553, wR2 = 0.1294 | R1 = 0.0958, wR2 = 0.2628 |
| Final R indexes [all data] | R1 = 0.1013, wR2 = 0.1487 | R1 = 0.1521, wR2 = 0.2974 |
| Largest diff. peak/hole / e Å-3 | 0.21/-0.22 | 0.66/-0.39 |

Table S2. Photophysical properties of DTP-ν-DABNA and DTPF-ν-DABNA.

| Solvent | DTPF-ν-DABNA |  | DTP-ν-DABNA |  |
| --- | --- | --- | --- | --- |
|  | λPL | FWHM | λPL | FWHM |
|  | nm | nm | nm | nm |
| n-Hexane | 466 | 18 | 474 | 18 |
| Toluene | 474 | 16 | 484 | 17 |
| 1,4-Dioxane | 473 | 17 | 482 | 18 |
| Tetrahydrofuran | 477 | 20 | 487 | 17 |
| Trichloromethane | 478 | 20 | 490 | 17 |
| Dichloromethane | 480 | 22 | 491 | 20 |
| N,N-Dimethylformamide | 481 | 20 | 490 | 21 |

Table S3. Photophysical properties DTP-ν-DABNA and DTPF-ν-DABNA in doped PPF films (2 wt%).

| Compound | ФPF/ФDF %/% | τPF/τDF ns/μs | kPF ×108 s-1 | kDF ×104 s-1 | krS ×108 s-1 | kISC ×107 s-1 | kRISC ×105 s-1 | knrS ×106 s-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DTPF-ν-DABNA | 67.4/31.8 | 3.40/11.66 | 2.94 | 8.58 | 1.98 | 9.41 | 1.26 | 1.60 |
| DTP-ν-DABNA | 53.4/42.1 | 2.98/13.15 | 3.36 | 7.60 | 1.79 | 14.8 | 1.36 | 8.44 |
| In this work, the doped films of DTP-ν-DABNA and DTPF-ν-DABNA do not exhibit phosphorescence emission at 300 K. In other words, the efficiency of phosphorescence is zero (ФPhos = 0). Thus, the quantum efficiency of delayed emission (ФDE) is equal to the efficiency of delayed fluorescence (ФDF). Thus, the quantum efficiencies of prompt (ФPF) and delayed emission (ФDF) are evaluated by the corrected estimation method and the rate constants were calculated according to the reported method[4]. kPF= 1τPF kDF= 1τDF krS= kPFΦPF knrS= kPFΦPFΦall(1− Φall) kISC= kPFΦDFΦall− kDFΦDFΦPF kRISC= kDFΦallΦPF knrT=0 where kPF and kDF are the radiative decay rate for prompt and delayed fluorescence, respectively, Фall is the total photoluminescence quantum efficiency, KrS and knrS are the radiative and nonradiative decay rate constants from a singlet excited state, respectively, kISC and kRISC are the intersystem crossing and reverse intersystem crossing rate constants, respectively, knrT is the nonradiative decay rate constant from a triplet excited state. |  |  |  |  |  |  |  |  |

Table S4. Summary of OLED device performance utilizing ν-DABNA, DTPF-ν-DABNA and DTP-ν-DABNA.

| Dopant | x (wt%) | CEmax/10/100/1000 (cd A-1) | PE max/10/100/1000 (lm W-1) | EQE max/10/100/1000 (%) |
| --- | --- | --- | --- | --- |
| ν-DABNA | 1 | 31.0/-/29.5/23.2 | 25.6/-/20.8/11.7 | 34.4/-/32.8/26.0 |
| DTPF-ν-DABNA | 2 | 40.0/33.7/22.8/7.8 | 40.5/33.1/19.3/4.4 | 36.0/28.9/18.5/6.3 |
|  | 5 | 40.0/33.7/21.3/6.6 | 40.4/32.8/17.8/3.4 | 34.2/27.3/18.2/5.7 |
|  | 10 | 30.0/27.3/18.6/5.9 | 30.4/26.5/15.6/3.0 | 24.6/21.2/14.6/4.6 |
| DTP-ν-DABNA | 2 | 50.0/44.7/34.8/16.2 | 50.0/43.2/28.8/9.9 | 31.5/27.0/20.9/9.1 |
|  | 5 | 44.9/44.2/33.7/14.5 | 43.7/42.9/28.2/8.5 | 25.6/25.1/19.1/8.7 |
|  | 10 | 40.0/34.6/28.6/13.5 | 40.8/33.8/24.1/8.0 | 22.7/18.8/15.4/7.4 |

Values of current efficiency (CE), power efficiency (PE), and external quantum efficiency (EQE) at the maximum, 10/100/1000 cd m-2

Table S5 Summary of reported diboron blue MR-TADF emitters with high efficiency (EQEmax > 30%).

| Emitters | λEL (nm) | FWHM (nm) | EQEmax (%) | CIE (x, y) | Ref. |
| --- | --- | --- | --- | --- | --- |
| DTPF-ν-DABNA | 480 | 21 | 36.0 | (0.09, 0.22) | This work |
| DTP-ν-DABNA | 492 | 22 | 31.5 | (0.07, 0.38) |  |
| CFDBCz | 488 | 22 | 32.4 | (0.12, 0.43) | Adv. Opt. Mater. 2024, 12(15):2302987. |
| ν-DABNA | 469 | 18 | 34.4 | (0.12, 0.11) | Nat. Photon. 2019, 13(10):678-682. |
| NO-DBMR | 469 | 26 | 33.7% | (0.12, 0.12) | Angewandte Chemie International Edition. 2023, 62(32):e202306768. |
| Π-CzBN | 494 | 21 | 37.4 | (0.08, 0.45) | Angewandte Chemie International Edition. 2023, 62(32):e202306413. |
| DTBA-B2N3 | 475 | 28 | 30.9 | (0.11,0.18) | Nat. Photon. 2023, 17(3):280-285. |
| o-Tol-ν-DABNA-Me | 472 | 18 | 33.1 | (0.11, 0.12) | Sci. Adv. 2023, 9(22):eadf1388. |
| m-ν-DABNA | 471 | 18 | 36.2 | (0.12, 0.12) | Chem. Eng. J. 2022, 432:134381. |
| 4F-ν-DABNA | 464 | 18 | 35.8 | (0.13, 0.08) |  |
| 4F-mν-DABNA | 461 | 18 | 33.7 | (0.13, 0.06) |  |
| m[B-N]N1 | 478 | 30 | 30.4 | (0.13, 0.27) | Angewandte Chemie International Edition. 2022, 61(40):e202207293. |

References

1.Wang C, Kang X, Dai S, Cui F, Li Y, Mu H, et al. Efficient suppression of chain transfer and branching via C(s) -type shielding in a neutral nickel(II) catalyst. Angew. Chem Int Ed. 2021;60(8):4018-4022. [DOI:10.1002/anie.202013069]

2.Schlütter F, Nishiuchi T, Enkelmann V, Müllen K. π-Congested poly(paraphenylene) from 2,2′,6,6′-tetraphenyl-1,1′-biphenyl units: synthesis and structural characterization. Polym Chem. 2013;4(10):2963-2967. [DOI:10.1039/c3py00166k]

3.Naveen KR, Lee H, Braveenth R, Yang KJ, Hwang SJ, Kwoin JH. Deep blue diboron embedded multi-resonance thermally activated delayed fluorescence emitters for narrowband organic light emitting diodes. Chem Eng J. 2022;432:134381. [DOI:10.1016/j.cej.2021.134381]

4.Tsuchiya Y, Diesing S, Bencheikh F, Wada Y, Santos PL, Kaji H, et al. Exact solution of kinetic analysis for thermally activated delayed fluorescence materials. J. Phys Chem Lett. 2021;125(36):8074-8089. [DOI:10.1021/acs.jpca.1c04056]