https://doi.org/10.70401/tx.2026.0027

Supplementary information

A cumulative model for thermoelectric cooling with temperature dependent material properties

Kang Zhu, Xuechun Li, Alex Brown, Rujie Shi, Hee Seok Kim, Weishu Liu

1.Derivation of the original cumulative model

This section presents the detailed derivation of the maximum COP and nondimensional cooling power density given by Eq. (3) in the original cumulative model. It starts from the one-dimensional governing equation of the thermal and electrical flow within a thermoelectric element in steady state,

ddxκTdTdx+J2ρT−JτTdTdx=0#S1

where J is the current density from the cold to hot side of the element, and x is the coordinate in parallel to J. By integrating Eq. (S1) twice with respect to x, the following equations are obtained,

κTdTdx+J20xρTdx−JTcTτTdT+C1=0#S2

TcTκTdT+J20x0xρTdxdx−J0xTcTτTdTdx+C1x+C2=0#S3

Applying the boundary conditions, T=Tc at x=0 and T=Th at x=L, to the above integral equations, where L is the length of the element, C1 and C2 are deduced as

C2=0#S4

and

C1=−κTcdTdxx=0=−1LTcThκTdT+J20L0xρTdxdx−J0LTcTτTdTdx#S5

Thus, the cooling power density, i.e., the heat flux at the cold side is given by

qc=−1LTcThκTdT+JSTcTc+1L0LTcTτTdTdx−J21L0L0xρTdxdx#S6

The electric power input is given by

P=ITcThSTdT+I2R#S7

where I=JA is the electric current and R=1A0LρTdx is the electric resistance of the element. Divided by the cross-sectional area A, the input power density is

Pdens=JTcThSTdT+J20LρTdx#S8

Prior to further derivation, the integral terms with respect to x are converted into those with respect to T assuming a linear relation between T and x,

0LρTdx=0LρTdxdTdT≈L∆TTcThρTdT#S9

0L0xρTdxdx≈L2∆T2TcThTcTρTdTdT#S10

0LTcTτTdTdx≈L∆TTcThTcTτTdTdT#S11

Introducing the nondimensional factors WJ and WT given by Eq. (5), the cooling power density and electric power density are rewritten as

qc=−1LTcThκTdT+JSTcTc+WTTcThτTdT−J2WJL∆TTcThρTdT#S12

Pdens=JTcThSTdT+J2L∆TTcThρTdT#S13

According to Eq. (S12), the maximum cooling power density is reached as

qc,max=−1LTcThκTdT+STcTc+WTTcThτTdT24WJL∆TTcThρTdT#S14

when

J=STcTc+WTTcThτTdT2WJL∆TTcThρTdT#S15

Substituting α0=TcSTc+WTTcThτTdTTcThSTdT into Eqs. (S14-15) and identifying 1LTcThκTdT to be the thermal conducting heat flux under ∆T, the expressions for the maximum nondimensional cooling power density and the corresponding electric current density are obtained,

qc, maxqcond=α024WJTcThSTdT2TcThρTdTTcThκTdTΔT−1=α024WJ(ZT)eng−1#S16

J=α0TcThSTdT2WJL∆TTcThρTdT#S17

The COP is obtained by dividing the cooling power density by electric power density,

COP=−1LTcThκTdT+JSTcTc+WTTcThτTdT−J2WJL∆TTcThρTdTJTcThSTdT+J2L∆TTcThρTdT#S18

Letting dCOPdJ=0, the maximum COP and the corresponding electric current density are deduced after some algebra,

COPmax=α01+α1(ZT)eng−α21+α1(ZT)eng+1#S19

J=∆TLTcThSTdTTcThρTdT11+α1(ZT)eng−1#S20

The αi terms (i = 0, 1, 2) are given by Eq. (4).

2.Refinement of the cumulative model

This section presents a refinement of the cumulative model based on a direct comparison between 0L'ρdx and L'ΔT'TcTh'ρdT. Assuming a linear relationship between the electric resistivity and temperature (which is not true for many TE materials over a relatively large temperature range, but it is sufficient in this context for a qualitative explanation),

ρ=ρ0+γT−Tc#S21

the integration of ρ over x is unfolded as

0L'ρdx=0L'ρ0+γT−Tcdx#S22

The temperature evolution along the TE element is approximated by

T=−ρJ22κx2+ρJ22κL+ΔTLx+Tc#S23

under the constant-property assumption. So Eq. (S22) can be further unfolded as

0L'ρdx=ρ0L'+γL'2−ρJ26κL'+12ρJ22κL+ΔTL#S24

And L'ΔT'TcTh'ρdT is unfolded as

L'ΔT'TcTh'ρdT=ρ0L'+γL'2−ρJ24κL'+12ρJ22κL+ΔTL#S25

According to Eqs. (S24) and (S25),

0L'ρdx=L'ΔT'TcTh'ρdT+112γL'3ρJ2κ#S26

From Eq. (S23) the location coordinate corresponding to the peak temperature is given by

L'=12L+κρJ2ΔTL#S27

Substituting it into Eq. (S26),

0L'ρdx=L'ΔT'TcTh'ρdT+196γL3ρJ2κ+112γκρJ22ΔTL3+116γLΔT+18γκρJ2ΔT2L#S28

Substituting Eq. (S28) into Eq. (9), the cooling power density is given by

qc=−J2L'ΔT'TcTh'ρdT+STcTc+TcTh'τdTJ−18γκρΔT2L−196γL3ρJ4κ−112γκρJ2ΔTL3−116γLΔTJ2#S29

Only the first three terms are reserved here, thus

qc=−J2L'ΔT'TcTh'ρdT+STcTc+TcTh'τdTJ−18γκρΔT2L#S30

And the maximum cooling power density is

qc, max=β02TcTh'SdT2ΔT'4TcTh'ρdTTcTh'κdT1L'TcTh'κdT−18γκρΔT2L#S31

Eq. (S31) is different from Eq. (13) by the additional term −18γκρΔT2L. The nondimensional maximum cooling power density is given by

qc, maxqcond=β024ZTeng'−18γκρΔT2LL'TcTh'κdT#S32

Substituting Eq. (7) into the above equation, and assuming κ≈1ΔT'TcTh'κdT, the following equation is obtained,

qc, maxqcond=β024ZTeng'−14γΔTρ112ZTc+ΔTTcΔTTc#S33

The above equation can be generalized into

qc, maxqcond=β024ZTeng'−β1ΔTTc#S34

to account for different temperature dependences of ρ. From the above derivation, Eq. (14) is refined into Eq. (S34) to account for the difference between 0L'ρdx and L'ΔT'TcTh'ρdT. In this work β1 is given by 0.6ρ'Tcρ'Th based on an observation and analysis of the prediction errors of Eq. (14). The key of the above derivation is to identify ΔTTc as a critical correction term, which is confirmed by the appreciable improvement in the accuracy of Eq. (17) over Eq. (14).

3.Some of the calculating results

Figure S1. Comparisons of predicted maximum COP by Eqs. (3a) and (1a) to numerical results (n = 5-8).

Figure S2. Comparisons of predicted maximum nondimensional cooling power density by Eqs. (3b) and (2) to numerical results (n = 5-8).

Figure S3. Comparisons of predicted maximum nondimensional cooling power density by Eqs. (12) and (14) to numerical results (n = 5-8).

Figure S4. Comparisons of predicted maximum nondimensional cooling power density by Eqs. (16) and (17) to numerical results (n = 5-8).

Figure S5. Physical properties of the commercial P and N type thermoelectric materials for sub-ambient cooling.